Section II: Experimentation

- Sensors and modificatons – specifications and data
- Aggregate Samples used
  - Specifications – mass, k, ISS, mass/volume ratio, average cobble volume, Fineness Modulus
- Calorimetry
  - Describe method and theory
- Stormwater discharge simulator (find a better name?)
  - Describe operation, design considerations, specifications
  - Identify terminology used for data and analysis
  - Flow sensor interface

Two seperate experiments were devised to measure thermal exchanges between water and a sample of gravel. First, calorimetry experiments were performed to determine the specific heat of a gravel sample in a hydrostatic environment. Secondly, a so-called stormwater discharge simulator was constructed to flush a body of gravel with heated water at reasonably high rates for up to 5 minutes. Temperature sensors, in both experiments, measured changes in water temperature and afforded an analysis of heat exchnge between water and gravel. In each group of experimental trials, a family of 9 gravel or rock samples was measured. (table below)
Sample ID	Description

Sample ID	Mass (kg)	ISS / Total Volume	Volume (L)	Cobbles / Litre

Temperature Sensors
The temperature sensors used were HOBO water temperature sensors manufactured by Onset Instruments. The sensors were in turn physically modified to achieve a responsivity on the order of a few seconds, as the conventional manufacturer specified responsivity was as large as 15 minutes for measurements within 1%. Sensors were then “matched” by submersing a family of 6-8 sensors in both hot and cold water reservoirs, and then selecting pairs of sensors that had the most similar temperature readings and the fastest responsivity. This matching process was performed each time for varied flow rates (low, medium and high) in the stormwater discharge simulator as well as the calorimetry experiements. (calibration figure example??)

Calorimetry
To experimentally determine the thermal conductivity and specific heat capacity of an aggregate, sample was immersed in a static mass of water. The water bath was initiated with a typical temperature of about 75 C, and the aggregate assumed the temperature of the environment, usually between 20 and 23 C. HOBO sensors were placed in the hot water bath and left to sit for several moments before the aggregate was indroduced to the water, so as to afford some time for stabilization in the sensor and fluid. Aggregate was then immersed into the water en mass, and after 15 minutes the sensors were removed for data collection. The resultant temperature data consistently featured a cooling curve that conveys information about the rate and quantity of thermal energy exchanged between the water and the aggregate. (figure)
To analyticlly model the heat transfer characteristics of an aggregate, and ultimately to empirically determine a bulk thermal conductivity and specific heat, we assume that:

- All material properties of the aggregate are constant. Although the aggregate may be comprised of variable materials, the mix of materials is thorough and homogenous, allowing the aggregate to be adequately represented through mean bulk material properties.
- All material properties of the aggregate are independent of temperature. Within the temperature ranges nominally encountered in this application, it is assumed that temperature variation of material properties is negligible.
- The Biot number is small (Bi<0.1), where the Biot number is defined as:

size 12{ ital "Bi"= { {αR} over {k} } } {}

where α is the heat transfer coefficient [W/m2/K], R is the characteristic radius of the aggregate [m], and k is the thermal conductivity [W/m/K]. A small Biot number implies that heat transfer rate is due solely to conduction and is immediate (λ→∞) within the aggregate body as compared to the heat transfer rate at the boundary such that the heat field within the body is homogenous and need not be resolved spatially. This assumption is recommended for calculating heat transfer rates of bodies with arbitrary shape (Baehr & Stephan, 2006)[]ref

To determine the change in temperature of the aggregate with time, we first consider the First Law of Thermodynamics:

size 12{ { { ital "dU"} over { ital "dt"} } = { dot {Q}}} {}	(1)

where U [J] is the internal energy of the aggregate and size 12{ { dot {Q}}} {} [W] is the heat flow across the composite boundary. If the aggregate of volume V has a density ρ [kg/m3] and specific heat capacity c [J/kg/K], then it holds that

size 12{ { { ital "dU"} over { ital "dt"} } =Vρ { { ital "du"} over { ital "dt"} } =Vρc { { ital "dT"} over { ital "dr"} } } {}	(2)

where u is the specific internal energy [J/kg] and r is the radial dimension [m] normal to the aggregate surface at any differential boundary location. If the composite surface area of the aggregate is A, we obtain:

size 12{ { dot {Q}}=αA left (T - T rSub { size 8{S} } right )} {}	(3)

and, from (1), we obtain:

size 12{ { { ital "dT"} over { ital "dt"} } = { {αA} over {cρV} } left (T - T rSub { size 8{S} } right )} {}	(4)

which has the solution

size 12{T - T rSub { size 8{S} } = left (T rSub { size 8{0} } - T rSub { size 8{S} } right )"exp" left ( - { {t} over {τ} } right )} {}	(5)

with time constant

size 12{τ= { {cρV} over {αA} } } {}
(6)

Because the calorimetry experiments performed produced exponential decay curves, the time constant can be determined from data regression. Since the density and volume for any given experiment may be determined from Archimedes’ methods and the surface area inferred from the fineness modulus provided by the manufacturer, the ratio c/α may be determined for each gravel aggregate material.
Additionally, the decay curve can be integrated to determine the cumulative volume of heat exchanged.